## Slide 1
Molecular Dynamics Simulation Study of the LCST Phase Transition Behavior of a Single PNVCL Chain in Aqueous Solution
Xinyue Zhang，Mingge Zhao, Junhan Cho
* Department of Polymer Science and Engineering, Dankook University
*Correspondence: jhcho@dankook.ac.kr
Abstract
Introduction
Light scattering results confirmed that phase separation occurs in PNVCL aqueous solution at approximately 32.1 °C.
Structural analysis using Rg and RDF showed that PNVCL transitions from an extended to a globular conformation around 305 K, which is consistent with the light scattering results.
RDF analysis revealed that hydrogen bonding between PNVCL and water molecules, as well as between water molecules themselves, decreases with increasing temperature. This supports the conclusion that hydrogen bonding plays a key role in the phase separation behavior.
Results and Discussion
Conclusion
Theory
This study investigates the temperature-dependent LCST phase behavior of a single poly(N-vinylcaprolactam) (PNVCL) chain in aqueous solution using molecular dynamics (MD) simulations. As a thermoresponsive polymer, PNVCL is widely applied in biomedical and smart material fields, with its LCST behavior being especially relevant near physiological temperatures.
MD simulations were performed using the OPLS-5 force field with temperature intervals of 10 K. Structural changes and phase behavior were analyzed through radius of gyration (Rg), hydrogen bonding, and radial distribution functions (RDF). Visual analysis further revealed temperature-driven interactions between PNVCL and water molecules.
These findings provide insights into the microscopic mechanism of PNVCL’s phase transition and offer theoretical support for its practical applications.
Keywords: PNVCL, Phase Behavior, Simulation, Molecular Dynamics，Lower Critical Solution Temperature, Molecular dynamics simulation
Introduction to Molecular Dynamics(MD) Simulation
Flory-Hggins Theory ---(type1)
Acknowledgment: National Research Foundation of Korea (Basic Science Research Program)
Introduction of Poly(N-vinyl caprolactam)
Sun, Xiaoquan. Structure and Property of Polymers and Biopolymers from Molecular Dynamic Simulations. University of Arkansas, 2018.
Molecular dynamics (MD) simulation is a computational method used to investigate the dynamic behavior of atoms and molecules in nanoscale systems. By numerically solving Newton’s equations of motion, it provides time-resolved atomic trajectories, enabling the analysis of structural and thermodynamic properties. MD has become an essential tool in materials science and molecular research, offering insights into processes that are often challenging to observe experimentally.
Synthetic route of PVCL via free radical polymerization from N-vinylcaprolactam(VCL)
Sun, Xiaoquan. Structure and Property of Polymers and Biopolymers from Molecular Dynamic Simulations. University of Arkansas, 2018.
The schematic workflow of MD simulation
Advantages:
1.Exhibits LCST behavior near body temperature in water.
2.Biocompatible and suitable for biomedical use.
3.Polymerization can be controlled via free-radical methods.
Challenge:
Controlled polymerization of NVCL is difficult due to its distinct properties, making copolymerization with other monomers more complex.
OPLS-5 Force Field
Both the addition of polarizability and new metals features are encompassed in a new model termed OPLS5
The OPLS5 functional form is given by:
E = EOPLS + ∑drudesKD(r-req)2
+∑metal complexes[EFLucCT+EAOM+EMorse]
EOPLS includes bond, angle, dihedral, van der Waals, and Coulomb interactions, with modified charge site definitions.
Damm, Wolfgang, et al. "OPLS5: Addition of Polarizability and Improved Treatment of Metals." (2024).
Visualization section
295K 1ns
295K 200ns
335K 1ns
335K 200ns
The visualization clearly shows the transition of PNVCL from a linear to a globular conformation.
PNVCL:25mer ----1 chain
Nwater:4200
wt%:4.4wt%
tacticity: syndiotactic
force field :OPLS5
simulation time:200ns
PNVCL(4.4wt%)
Both light scattering experiments and MD simulations indicate that phase separation occurs around 305 K.
Light scattering experiments + MD simulations
radius of gyration
end-to-end distance
300K Rg
305K Rg
315K Rg
A significant decrease in the radius of gyration is observed at 305 K.
Radial distribution functions + H-bond
Based on the peak position and sharpness, the interaction between water molecules and carbonyl oxygen is significantly stronger. The RDF results indicate that hydrogen bonding plays a crucial role in the phase separation process of PNVCL.
H-bonds
It can be observed that the total number of hydrogen bonds decreases with increasing temperature.